## Slide 1: Ion irradiation effects on multiwalled carbon nanotubes structure

## Slide 2
Prepared by
Emad Mahmoud Elsehly
Lecture assistance, Damanhur University, Egypt
PhD Student in SINP MSU, Russia
Supervisors
Prof. N. G. Chechenin
SINP MSU, Russia
Prof. H. A. Motaweh
Damanhur University, Egypt

## Slide 3: Objectives
Investigate the modification Multiwalled Carbon nanotubes (MWNTs) using He ion irradiation.
Characterization of ion beam irradiated MWNTs using (SEM and Raman spectrometry).
Study the modification mechanisms of irradiated MWNTs.
Work importance
Investigations on structural change of irradiated CNTs are of great importance to provide insights for interactions between energetic particles and CNTs.
The ion beam not only is used to control defects in nanotubes but also change the tubes diameter which enhances their performance for various potential applications like water filtration.

## Slide 4
1. INTRODUCTION
Carbon nanotubes
high surface areas
smaller pores with high permeability
good mechanical and thermal stability
energy saving and low cost
High adsorption capacity
Properties
Applications
Composites
Electronics and batteries
Water purification
Solar cells
Space devices
Carbon nanotubes are allotropes of carbon. These cylindrical carbon molecules have interesting properties that make them potentially useful in many applications, There are different shapes: MWNTs and SWNTs
MWNT
SWNT

## Slide 5: How CNTs are made
1) Arc discharge
  CNTs Can be found in the carbon soot of graphite electrodes during an arc discharge involving high current.
2) Laser Ablation
  In the laser ablation process, a pulsed laser vaporizes a graphite target in a high-temperature reactor while an inert gas is inserted into the reactor. Nanotubes develop on the cooler surfaces of the reactor as the vaporized carbon condenses.
  Other methods where CNTs are created:
  Chemical Vapor Decomposition (CVD)
  (Our laboratory method)

## Slide 6: Synthesized MWNT arrays using CVD method
A liquid solution of ferrocene in cyclohexane as soon as the support nitrogen gas were supplied into the Ø 2.5 cm × 100 cm long quartz tube placed in an automatically temperature controlled oven. With the described method uniform forest arrays up to of 20 × 80 mm2 were systematically obtained on silicon substrate.
(Our laboratory method in SINP, MSU)

## Slide 7
“Taunit-MD” | “Taunit-M” | Parameter/CNTs
(30-50) | (10-20) | External diameter, nm
(10-20) | (4-8) | Internal diameter, nm
20 and more | 2 and more | Length, µm
(179) | 240 | Specific surface area, m2/g
0.06 | 0.05 | Bulk density, g/cm3
Commercial MWCNTs (powder)
Taunit-M
Taunit-MD
The industrial carbon nanotube “Taunit-M” and “Taunit-MD” CNTs produced by “Nanotech Center” (Tambov, Russia) in a form of powder, composed of grainy agglomerates of MWNTs.

## Slide 8
Purification and functionalization of Carbon nanotubes
As-prepared MWNTs contain a variety of impurities, such as amorphous carbon, metallic catalyst.
The surface of carbon nanotubes is originally inert and solvophobic
These problems limits the best performance of CNTs for practical applications like water filtration.
A possible solution to these problems is to modify the surface of carbon nanotubes by different treatments techniques:
Modification
Chemical acids
Electron beam irradiation
Ion beam irradiation
SEM
Raman spectrometry

## Slide 9
Scanning electron microscope
HNO3
oxidation
1) Chemical treatment
Raman spectroscopy
Pristine
HCl+ H2O2
HNO3
Elsehly, E. M., Chechenin, N. G., Makunin, A.V., Motaweh, H. A., Vorobyeva, E.A., et al. 2016 Characterization of functionalized multiwalled carbon nanotubes and application as an effective filter for heavy metal removal from aqueous solutions. Chinese Journal of Chemical Engineering, In press [doi: 10.1016/j.cjche.2016.05.017]

## Slide 10
2) Electron beam irradiation
Samples | ID /IG | ID′ /IG | ID /IG′
Raw MWNTs | 1.07 | 0.39 | 1.8
Annealed MWNTs | 0.74 | 0.27 | 0.9
D1=60 nm
D2=70 nm
D1=50 nm
D1=30 nm
Elsehly E M, Chechenin N G, Makunin A V and Motaweh H A 2016 Morphological and structural modifications of multiwalled carbon nanotubes by electron beam irradiation Material research express 3 105013
Impurities
(amorphous carbon)
Clear tubes with reduced diameter

## Slide 11: Vacancies (V) Adatoms (A)
3) He ion beams to modify properties of carbon nanotubes
The irradiation of CNTs by 80 keV He ion beam can produce clear changes in morphology of the surface, increases defects concentration and finally leads to amorphization.
We explore the defect formation in MWNTs pressed samples caused by He ions irradiation with different doses.
The irradiation effects are characterized using scanning electron microscopy (SEM) and Raman spectroscopy.
The thermal and athermal mechanisms of the irradiation effects are discussed.

## Slide 12: Preparations & Methods
The pressed tablets of MWNT taunit and arrays were irradiated at HVEEE-500 ion accelerator at SINP MSU with He ion beam of the energy E= 80 keV with fluencies 1x1016, 2x1016 and 7x1016 ion/cm2.
The residual pressure in the chamber during the test did not exceeded 2x10-4 Pa. The sample temperature during the ion irradiation did not exceed 1oC.
Purified Taunit-M and Taunit-MD were compressed using high pressure piston to the form of circular tablet with the diameter 20 mm and the thickness of 2 to 4 mm.
Ion Beam Laboratory Irradiation Facility
SINP (MSU)

## Slide 13: Characterization of irradiated MWNTs (SEM)
The structure and composition of the pristine and irradiated MWNT samples were studied by SEM and the average diameter distribution of nanotubes were obtained with the SEM image analyzer.
Taunit-M
Average diameter = 19 nm
Average diameter = 15 nm
Ion irradiation

## Slide 14
Taunit-MD
Ion irradiation
Average diameter = 36 nm
Average diameter = 22 nm
SEM pictures of two samples, one pristine and the other irradiated by He ions with the fluence of 1x1016 ions/cm2
These numbers show that the irradiated MWNTs, on the average, have lost their outermost walls followed by some amorphous structure.

## Slide 15: Characterization of irradiated MWNT arrays (SEM)
Average diameter=80 nm
Average diameter=60 nm
pristine
Irradiated
1x1016
Fluence
Large diameter
small diameter
More defective
More crystalline

## Slide 16
Characterization of irradiated Taunit-MD (Raman)
Three characteristic peaks, the D band (disorder band of sp3-hybridized carbon), the G band (graphite band of sp2-hybridized carbon) and the G′ band (second overtone of the defect induced D band and is related to the three dimensional order) appeared at 1340, 1580and 2700 cm-1, respectively. These peaks are important for determining the graphitic nature and structural ordering of the tubes
The structure defects were characterized by analysis of Raman spectra which were measured using micro Raman NTEGRA Spectra system with 473 nm excitation laser wavelength
The figure shows an increasing in ID/IG ratio after ion beam irradiation, indicating increasing of defects and vacancies in irradiated sample. The band G′ supports our explanation: the higher intensity of G′-band accounts for fewer defects in non-irradiated CNTs, reduced G′ intensity after irradiation accounts for the defect formation.
before
after
80 keV He ion irradiation with fluence 1x1016 ions/cm2

## Slide 17: Dependence of Raman spectrum on irradiation fluence
From the figure, it was evident that the relative intensity of the D to G bands increases with enhancement of the irradiation dose followed by disappearing of G′-band.
At fluence 2x1016 ions/cm2, the structure of MWNTs became more disordered, due to the destruction of some walls of the tubes.
For further increasing of the fluence up to 7x1016 the amorphization of MWNTs appears.
These observations demonstrate that the ion beam dose is important to control the defect formation and transformation of the CNTs to amorphization state
Pristine
1x1016 ion / cm2
2x1016 ion / cm2
7x1016 ion / cm2
Elsehly E M, Chechenin N G, Makunin A V, Motaweh H A and Shemukhin A A 2016 He ion irradiation effects on multiwalled carbon nanotubes structure, in Proceeding of Many Particle Spectroscopy of Atoms, Molecules, Clusters and Surfaces Conference.

## Slide 18
Characterization of irradiated MWNT arrays (Raman)
The spectra of MWNTs has two characteristic peaks, D- peak at 1332 cm -1 and G- peak at 1600 cm -1.
During irradiation peaks become more widely, also, with the dose 2x1016 the structure it is practically completely amorphous.
Thus, it is possible to draw the conclusion that the ions create defects during irradiation, destroying the crystal structure of tube.

## Slide 19
Roughly, two alternative mechanisms, thermal and athermal, can be suggested to explain the reduction of the CNTs diameter.
The contribution of the athermal mechanism connected with the physical sputtering of the outermost layers of the CNTs. The following estimations will show that this contribution is negligible even for the highest fluence applied (1x1016 ions/cm2).
Alternatively, the deposited energy of ion could go to the heating the nanotube under ion bombardment. The estimations shows the unrealistic temperature of T~ 2.2∙106 K . This means that other channels work for the dissipation of the deposited ion energy. One of them is dissipations of the heat through the contacts with neighboring tubes.
Diameter reduction mechanism

## Slide 20
1) Estimation of the contribution of the physical sputtering as an athermal mechanism of the CNTs diameter reduction induced by ion beam radiation
Physical sputtering can be considered as a potential reason of the reduction effect.
Assuming that the sputtering yield Y , the number of sputtered carbon atoms per ion is equal to 0.01, the same as in graphite. The number of sputtered layers nsl in CNT can be determined as
nsl = (Di∙Y)/nCl, nCl = 2/Ahex
Di is the ion dose and nCl is the C-atoms density at the outer surface of the CNTs. nCl can be roughly estimated as inversely proportional to the area Ahex of the basal aromatic hexagon cell with 2 C atoms per cell and with spacing a = 0.141 nm between neighboring atoms, i.e.,
nCl ≈ 2/((33/2/2)∙(0.141∙10-7)2) ≈ 7.5∙1014.
nsl = 1∙1016∙0.01/7.5∙1014 ≈ 0.13 of layer,
meaning that there is no contribution of athermal physical sputtering in the tube diameter reduction.

## Slide 21
When passing through the tube lying perpendicular to an ion path, the ion loses the energy
ΔE ≈ (dE/dx)∙d∙f,
where d is the CNT diameter and f is a correction factor is equal to 2/π.
Assuming, that the ion energy loss is the same as in graphite for 80 keV He we get
dE/dx ≈ 260 eV/nm and ΔE ≈ 5.8 keV for the tube of d=35 nm.
The total energy deposited by the ion beam with the tube length l ~ 50 μm
E ~ ΔE∙Di∙d∙l ≈ 1∙1012 eV=1.6∙10-7 J.
Normally, the part of the ion energy deposited in the materials is transferred into heat, spreads over the samples and leaks away into surroundings.
In the case of CNTs situation differs from the common one by the fact of a high thermal conductivity along the tubes. If we assume a limiting case that all the energy deposited in a tube is kept within the tube, then the increase of their temperature
T= E/(m∙C)
Where the CNT mass m ≈ π (d/2)2lρ ~10-13g,with ρ ≈2.2 g∙cm-3, as well as specific heat C ≈ 0.74 J/(gK), were taken as for graphite.
This gives the T~2.2∙106 K, which is, of course, unrealistic temperature, suggesting an important role of other channels of energy dissipation.
2) Estimation of the contribution of the ion beam induced heating effect
Notes: f is a correction factor which takes into account the passing chord in the tube cross-section is smaller than the diameter in average

## Slide 22
Elsehly, E.M., Chechenin, N.G., Bukunov, K.A., Makunin, A.V., Priselkova, A.B., Vorobyeva, E.A., & Motaweh, H.A. 2016a Removal of iron and manganese from aqueous solutions using carbon nanotubes filters. Water Science & Technology: Water Supply, 16, 347-353.
Schematic for the steps of irradiated MWNTs filters design and filtration mechanism

## Slide 23: Conclusions
We have studied the effect of irradiation of He ion beam of energy 80keV on compressed samples of MWNT Taunit and arrays.
Raman spectra used as powerful technique to investigate the formation of defects on the tube walls of irradiated MWNTs. As we proceeded to higher fluences, amorphization of the MWNTs dominated.
From SEM data we found that on average the outer diameters of the irradiated tubes are reduced indicating that MWNTs lose their outer walls as a result of irradiation. Thus, it is possible to systematically peel off the outermost wall of MWNTs taking incident beam at controlled values of ion fluence.
Further work at smaller steps of fluence will be useful to strengthen this belief and quantify the fluence values which can be used to systematically destroy outer layers.
A rough analysis showed that the radiation induced thermal heating can play an important role in stimulating the reduction of the CNT walls.
Controlling the defect formation in CNTs is promising material for different potential applications.