## Slide 1
Magnetic phenomena in intermetallic compounds RCo2: studies of the limits of the itinerant electron metamagnetism concept
D.P. Kozlenko, E. Burzo, S.E. Kichanov, P. Vlaic,
A.V. Rutkauskas, E.V. Lukin, B.N. Savenko

## Slide 2
The intermetallic compounds R-Co
Giant magnetoresistance effects
Magnetocaloric effects
Magnetoelastic effects
Structural phase transitions
Magnetic phase transitions
Permanent magnets
Magnetocaloric devices
Magnetoresistive data storage and recording
Technological applications
Strong correlated systems:
charge, structural, spin
Physical phenomena

## Slide 3
Non-magnetic R-ions:
YCo2 or LuCo2
MR = 0 μB
MCo = 0 μB
Paramagnetic state
up to 70-75 T
A metamagnetism of compounds R-Co
Magnetic R-ions:
TbCo2, HoCo2, ErCo2, DyCo2
MR = 6-10 μB
MCo = ~1 μB
R
R
Co

## Slide 4
A pressure effect on the metamagnetism of RCo2 compounds
J. Phys. Condens. Matter 19, 036213 (2007).
Phys. Rev. B 57, 2904 (1998).
E. Burzo, Repts. Progr. Phys. 61, 1099 (1998).
P

## Slide 5
DN-12 diffractometer for studies of microsamples (~ 1 mm3)
Advantages of IBR-2 pulsed neutron source for development of neutron scattering techniques under extreme conditions
Neutron diffraction at high pressure: structure aspects of magnetic properties origins
Lattice parameters, bond lengths and valence angle
Magnetic moments of R and Co
DN-6 diffractometer for high pressure studies (~ 0.001 mm3)

## Slide 6
The neutron scattering techniques under extreme conditions
Maximum pressure is 8 GPa =80 000 atm
Maximum pressure is 40 GPa =400 000 atm

## Slide 7
Theoretical calculations: the ground state electronic structures and magnetic properties of RCo2 compounds, the exchange and correlation energy
A pressure effect on the metamagnetism of RCo2 compounds
Neutron diffraction data: lattice parameters, bond lengths and valence angle, magnetic moments of R and Co

## Slide 8
A pressure effect on the crystal and magnetic structure of TbCo2
Theoretical dependences of Co9e and Co3b magnetic moments aon lattice parameters, describing pressure effect.

## Slide 9
A pressure effect on the crystal and magnetic structure of TbCo2
Temperature dependencies of Tb and Co ordered magnetic moments at selected pressures
Tb
Tb
Co

## Slide 10
A pressure effect on the crystal and magnetic structure of DyCo2

## Slide 11
A pressure effect on the crystal and magnetic structure of HoCo2
HoCo2
The theoretically calculated dependence of Co8c magnetic moments and of Ho5d band polarizations, as function of (a,c) lattice parameters of I41/amd structure.

## Slide 12
Neutron diffraction patterns of ErCo2 compound, measured at selected pressures and temperatures and processed by the Rietveld method.
The parts of neutron diffraction patterns measured at P = 2.1 GPa and T = 10 K, and calculated profiles for fixed Er magnetic moment MEr = 9.0 B and two values of Co magnetic moments MCo = -0.7 B and 0.0 B.
A pressure effect on the crystal and magnetic structure of ErCo2
Er (6c)
Co(9e)
Co(3b)
ka= 0.0007(1) GPa-1
kc=0.0055(5) GPa-1
A strong anisotropy in baric changes in interatomic bonding

## Slide 13
-3.5 K/GPa
A pressure effect on the crystal and magnetic structure of ErCo2
Er (6c)
Co(9e)
Co(3b)

## Slide 14
A pressure effect on the crystal and magnetic structure of RCo2
The dependence of cobalt moments at T=0 K on relative volume change.
The cobalt moments collapse
The magnetic moments of R is pressure invariant
The pressure induced cobalt moments collapse

## Slide 15
The limits of the itinerant electron metamagnetism concept
Tb
Tb
Co
Tb
Tb
Co
Non-magnetic R-ions:
YCo2 or LuCo2
Paramagnetic state
up to 70-75 T

## Slide 16
[1] D. P. Kozlenko, E. Burzo, P. Vlaic, S. E. Kichanov, A. V. Rutkauskas & B. N. Savenko “Collapse in ErCo2:Beyond the Limits of Itinerant Electron Metamagnetism” Sci. Rep. 5, 8620 (2015)
[2] E. Burzo, P. Vlaic, D.P. Kozlenko, S.E. Kichanov, N.T. Dang, A.V. Rutkauskas, B.N. Savenko “Magnetic properties, electronic structures and pressure effects of HoxY1-xCo2 compounds” Journal of Alloys and Compounds 584, 393–401 (2014).
[3] E. Burzo, P. Vlaic, D.P.Kozlenko, S.E.Kichanov, N.T. Dang, E.V.Lukin, B.N.Savenko “Magnetic properties of TbCo2 compound at high pressure” Journal of Alloys and Compounds V. 551, 702–710 (2013)
[4] E.Burzo, P. Vlaic, D.P.Kozlenko, “PRESSURE EFFECTS ON THE MAGNETIC BEHAVIOR OF COBALT IN RARE-EARTH COMPOUNDS” Rom. Journ. Phys. 60, 200-214 (2015).
[5] E. Burzo, I. Pop, D.P. Kozlenko, “Magnetic and magnetocaloric properties of some ferrimagnetic compounds” J. Optoelectron. Adv. Materials 12, 1105 (2010).
A pressure effect on the crystal and magnetic structure of RCo2
Encouraging Diploma for high-quality poster: “The high pressure studies of RCo2 compaund” – 2014
Frank Laboratory of Neutron Physics award 2015 "Magnetic phenomena in RCo2 intermetallides: investigation of the applicability limits of the concept of itinerant electron metamagnetism" I prize
Joint Institute for Nuclear Research award 2016 “Magnetic phenomena in intermetallic compounds RCo2: studies of the limits of the itinerant electron metamagnetism concept” I prize

## Slide 17
Thank you for your attention!