## Slide 1: Np-237 transmutation effectiveness dependence on beam particle and energy in QUINTA setup
S. Kilim, E. Strugalska-Gola, M. Szuta, S.I. Tyutyunnikov, J. Adam, V.I. Stegajlov

## Slide 2: Some Np-237 introductory data
Radioactive, T1/2 = 2.144106 y
Produced in a reactor as a nuclear waste.
Difficult to burn in PWRs. It accumulates.

## Slide 3: Basic Np-237 interaction modes with neutrons
Basic Np-237 interaction modes with neutrons
Np-237 fission and neutron capture CS dependence on energy
Neutron capture produces another actinide. Np-237 fission is in fact the only way to get rid of its long lived activity. High energy neutrons needed to make fission prevail over capture.

## Slide 4: QUINTA setup core vertical-axial cross section and 3D view

## Slide 5: Experiment data
*Particles: p – proton, d – deuteron, C6+ - carbon
Beam energy/particle* | 0.66 GeV/p | 2 GeV/d | 4 GeV/d | 8 GeV/d | 24 GeV/C6+ | 0.66 GeV/p | 
Date | 08 Nov 2014 | 04 Dec 2012 | 13 Dec 2012 | 22 Dec 2012 | 18 Dec 2013 | 22 Jun 2017 | 
Irradiation time (h) | 5.72 | 6.27 | 9.35 | 16.17 | 22.8 | 5.25 | 
Total number of beam particles | 8.64x1014 | 3.052(9)x1013 | 3.569(15) x1013 | 1.390(8) x1013 | 1.75 x1011 | 7.78(9)x1014 | 
Sample position | Left side window | Left side window | Left side window | Left side window | Left side window | Top of section 2 | Top of section 4
During the 22.06.2017 experiment the Np-237 samples were located on top of section 2 and section 4 of QUINTA while during the remaining ones in the left side window in lead shield.
During the 22.06.2017 experiment QUINTA was configured without lead shield.

## Slide 6: Experimental data work-out details
If – actinide fission rate, per deuteron and per gram
 – gamma line index
f – reaction index (f = fission)
S – gamma peak area
f – isotope production yield [%]
m – activation sample mass [g]
p – gamma spectrometer efficiency
I – gamma line intensity [%]
 - deuteron beam integral
COI – correction for gamma quanta coincidence
k – isotope decay constant
t+ – cooling time
tir – irradiation time
treal – real time of measurement
tlive – live time of measurement

## Slide 7: Experimental data work-out details
If – actinide fission rate, per deuteron and per gram
 – gamma line index
f – reaction index (f = fission)
S – gamma peak area
f – isotope production yield [%]
m – activation sample mass [g]
p – gamma spectrometer efficiency
I – gamma line intensity [%]
 - deuteron beam integral
COI – correction for gamma quanta coincidence
k – isotope decay constant
t+ – cooling time
tir – irradiation time
treal – real time of measurement
tlive – live time of measurement
Example detector efficiency function
εp = 2.0027x5 + 1.0373x4 - 1.0403x3 - 1.0105x2 + 0.3977x - 9.5181
x = ln(Eg)
R² = 0.8745

## Slide 8: Basic Np-237 FP identified decay chains – part 1/2

## Slide 9: Basic Np-237 FP identified decay chains – part 2/2

## Slide 10: Basic gamma lines identified
E-gamma, keV | Isotope | Source | T1/2 | Fission yield [%] [5] | I-gamma [%] [4]
529.87 | I-133 | FP | 20.87h | 6.46 | 87
658.08 | Zr-97->97Nb* | FP | 16.744h | 6.11 | 98.23
667.71 | Te-132->I-132** | FP | 3.26d | 4.85 | 98.7
743.36 | Zr-97 | FP | 16.744h | 6.11 | 93.6
772.6 | Te-132->I-132** | FP | 3.26d | 4.85 | 75.6
1131.51 | I-135 | FP | 6.57h | 6.71 | 22.6
1260.41 | I-135 | FP | 6.57h | 6.71 | 28.7
923.98 | Np-238 | CP | 2.117d | N/A | 2.869
962.77 | Np-238 | CP | 2.117d | N/A | 0.702
984.45 | Np-238 | CP | 2.117d | N/A | 27.8
1025.87 | Np-238 | CP | 2.117d | N/A | 9.65
1028.54 | Np-238 | CP | 2.117d | N/A | 20.38
FP – fission product. CP – neutron capture product.
*Line 658.08 keV stems in fact from Nb-97 beta decay (T1/2 = 72.1 min), but its quantity is modified by Zr-97 decay rate (T1/2 = 16.744h) [4]. Therefore Zr-97 decay constant (16.744h) approximates the line 658.08 activity decreasing.
**Lines 667.71 and 772.6 keV stem from I-132 (T1/2 = 2.295h) but their activities are modified by Te-132 decay rate (T1/2 = 3.26d) [4]. Therefore Te-132 decay constant (3.26d) approximates the lines activity decreasing.

## Slide 11: Np-237 fission and capture rate example partial results put together – experiment with 0.66 GeV proton beam
Np-237 sample located in QUINTA’s left side window in lead shield

## Slide 12: Np-237 fission and capture rate example partial results put together – experiment with 0.66 GeV proton beam
Np-237 sample located on top of section 4.

## Slide 13: Np-237 fission and capture rate example partial results put together – experiment with 0.66 GeV proton beam
Np-237 sample located on top of section 2.

## Slide 14: Np-237 fission and capture rate results dependence on beam particle, beam ion energy at sample location – QUINTA’s left side window
Legend: reaction/particle – for example F/p – fission/proton.
Reactions: F – fission, C – neutron capture.
Particles: p – proton, d – deuteron, C6+ - carbon 6-times ionized

## Slide 15: Np-237 fission and capture rate dependence on sample location for proton beam

## Slide 16: Np-237 fission to capture ratio dependence on beam particle and energy

## Slide 17: Np-237 fission to capture ratio dependence on sample location for proton beam

## Slide 18: Basic Np-237 incineration parameters for each experiment
Particle energy/particle \ Avg. fission and capture | 0.66GeV/p | 2GeV/d | 4GeV/d | 8GeV/d | 24GeV/C6+ | 0.66GeV/p/TS2 | 0.66GeV/p/TS4
fission (10-5 g-1p-1) | 1.67(35) | 5.56(87) | 8.95(12) | 13.3(24) | 51.08(135) | 1.38(25) | 1.28(30)
capture (10-5 g-1p-1) | 2.40(42) | 10.10(43) | 20.40(14) | 22.6(14) | 86.06(84) | 1.75(36) | 1.85(33)
fission (10-5 g-1p-1nucleon-1) | 1.67(35) | 2.78(43) | 4.47(60) | 6.65(12) | 4.26(11) | 1.38(25) | 1.28(30)
capture (10-5 g-1p-1nucleon-1) | 2.40(42) | 5.22(22) | 10.21(71) | 11.31(7) | 7.17(7) | 1.75(36) | 1.85(33)
fission (10-5 g-1p-1nucleon-1GeV-1) | 2.53(53) | 1.39(22) | 1.12(15) | 0.83(15) | 0.18(5) | 2.09(38) | 1.93(46)
capture (g-1p-1nucleon-1GeV-1) | 3.63(63) | 2.61(11) | 2.55(18) | 1.41(9) | 0.30(3) | 2.64(54) | 2.81(49)
fission (10-5 g-1p-1proton-1GeV-1) | 2.53(53) | 2.78(43) | 2.24(30) | 1.66(30) | 0.35(9) | 2.09(38) | 1.93(46)
capture (10-5 g-1p-1proton-1GeV-1) | 3.63(63) | 5.22(22) | 5.11(35) | 2.83(18) | 0.60(6) | 2.64(54) | 2.81(49)
F/C | 0.70(19) | 0.53(9) | 0.44(7) | 0.59(11) | 0.59(17) | 0.79(22) | 0.69(20)
F/A | 0.41(11) | 0.35(6) | 0.30(5) | 0.37(7) | 0.37(11) | 0.44(12) | 0.41(12)
TS2 – top of section 2. TS4 – top of section 4 of QUINTA.
Remainding – sample in side window in lead shield
Notes:
Experiments with samples at TS2 and TS4 position – QUINTA with no lead shield. The remaining – QUINTA in lead shield.
Experiments with 0.66 GeV proton beam (0.66 GeV/p, 0.66 GeV/p/TS2, 0.66 GeV/p/TS4) - both fission and capture rate and fission to capture ratio are very close to each other.

## Slide 19: Conclusions
Fission rate per beam energy unit suggests proton beam to be the best one for Np-237 incineration. It suggests that neutron contained in beam particle nucleus gives much less contribution than proton to target nuclei spallation.
The presented data show transmutation rate dependence on beam energy, but it is impossible to state where the maximum is.
For fixed beam particle (proton) and beam energy the incineration rate shows no dependence on Np-237 position. Fission to capture ratio shows no dependence on sample position what suggests the neutron spectrum to be uniform throughout entire QUINTA body.

## Slide 20: References
S. Kilim et al.; Np-237 incineration study in various beams in ADS setup QUINTA; Nukleonika 63, 17–22, 2018, https://doi.org/10.1515/nuka-2018-0003
W. Furman et al.; Recent results of the study of ADS with 500 kg natural uranium target assembly QUINTA irradiated by deuterons with energies from 1 to 8 GeV at JINR NUCLOTRON; PoS(Baldin ISHEPP XXI)086.
S. Kilim et al.; Measurements of Np-237 incineration in ADS setup QUINTA; PoS(Baldin ISHEP XXII)056
Evaluated Nuclear Data File (ENDF). Interpreted ENDF file. Np-237(FY_cum) Cumulative Fission-Product Yields and (n, ind_Fy) Independent Fission-Product Yields.
TABLE OF ISOTOPES, 8E
L. Zavorka et al. (2015); Neutron-induced transmutation reactions in 237Np, 238Pu, and 239Pu at the massive natural uranium spallation target; Nuclear Instruments and Methods in Physics Research B 349 (2015) 31–38; Retrieved September 14, 2015 from http://dx.doi.org/10.1016/j.nimb.2014.12.084; 0168-583X/_ 2015 Elsevier B.V.
S. R. Hashemi-Nezhad et al. “Optimal ion beam, target type and size for accelerator driven systems: implications to the associated accelerator power,” Ann. Nucl. Energy 38, 1144–1155 (2011).